Tremco, Inc. Commercial Sealants and Waterproofing

Section 09 67 00 FLUID-APPLIED FLOORING

Specifier: This guide specification section specifies TREMCO Sealer 200, a medium-duty UV stable Aliphatic Polyurethane topcoat applied over repaired and primed concrete, urethane cement and epoxy systems. This clear gloss sealer is color stable with good stain, chemical and impact resistance qualities.

This section is easily edited using several common commercial specification software tools.

We recommend you consult with your Tremco technical representative, who can be contacted through: Tremco, Inc., Commercial Sealants and Waterproofing Division, Beachwood OH; (866) 321-6357); email: techresources@tremcoinc.com;  www.tremcosealants.com.

Tremco sealant and waterproofing products appear in the following CSI MasterFormat specifications sections:

• Section 07 01 91 Joint Sealant Rehabilitation and Replacement
• Section 07 14 13.01 Hot Fluid-Applied Waterproofing, Deck (TREMproof 6100)
• Section 07 14 13.02 Hot Fluid-Applied Waterproofing, Vegetated Roof (TREMproof 6100)
• Section 07 14 16.01 Cold Fluid-Applied Waterproofing, Vertical and Deck (TREMproof 250GC)
• Section 07 14 16.02 Cold Fluid-Applied Waterproofing, Vertical (TREMproof 250GC)
• Section 07 14 16.03 Cold Fluid-Applied Waterproofing, Deck (TREMproof 250GC)
• Section 07 14 16.04 Cold Fluid-Applied Waterproofing, Vegetative Roof (TREMproof 250GC)
• Section 07 17 00 Bentonite Waterproofing (Paraseal GM/LG 60 mil)
• Section 07 18 00.01 Traffic Coatings, Vehicular
• Section 07 18 00.02 Traffic Coatings, Pedestrian
• Section 07 18 00.03 Traffic Coatings, Vehicular and Pedestrian
• Section 07 27 13 Modified Bituminous Sheet Waterproofing, Vapor-Retarding (ExoAir 110)
• Section 07 27 23 Board Product Waterproofing, Vapor Permeable (SECUREROCK ExoAir 430)
• Section 07 27 26.01 Fluid-Applied Membrane Waterproofing, Vapor-Retarding (ExoAir 120)
• Section 07 27 26.02 Fluid-Applied Membrane Waterproofing, Vapor Permeable (ExoAir 220)
• Section 07 27 26.03 Fluid-Applied Membrane Waterproofing, Vapor Permeable (ExoAir 230)
• Section 07 84 13 Penetration Firestopping
• Section 07 84 46 Fire-Resistive Joint Systems
• Section 07 92 00 Joint Sealants
• Section 08 85 00 Glazing Sealants
• Section 32 13 73 Concrete Paving Joint Sealants

TREMproof®, ExoAir®, Spectrem®, Tremflex®, Dymeric®, and Proglaze® are registered trademarks of Tremco, Inc.
This document is Copyright© 2014 by Tremco, Inc.

SECTION 09 67 00 – Fluid Applied Flooring

GENERAL

SUMMARY

Section Includes:

Architectural Solid Coatings of the Following Types: Sealers

RELATED REQUIREMENTS

Specifier: If retaining this optional Related Requirements Article, edit to include only those sections included in project manual.

Section 03 31 00 "Cast-in-Place Concrete" for moisture curing of concrete waterproofing substrate.

Section 03 39 00 “Concrete Curing” for moisture curing of concrete waterproofing substrate.

Section 03 63 00 “Epoxy Grouting”

Section 04 20 00 "Unit Masonry" for compatibility with flashing components.

Section 05 10 00 "Structural Metal Framing"

Section 05 50 00 “Metal Fabrications”

Section 07 90 00 "Joint Protection” for joint sealants and accessories and joint preparation.

Division 07 air barrier section for wall waterproofing and interface coordination.

Section 07 72 73 "Membrane Leak Detection System" for requirements for EFVM leak detection system installation and membrane leak testing.

Section 07 92 00 "Joint Sealants" for joint sealants and accessories and joint preparation.

Section 07 90 00/07 95 00 "Expansion Control/Protection" for expansion joint systems.

Section 33 46 00 "Subdrainage" for drainage pipe and conduits, drainage panels, and filter fabrics.

Section 09 90 00 “Painting and Coating”

Section 09 67 00 “Fluid applied Flooring”

Section 09 67 23 “Resinous Flooring” for additional fluid applied flooring materials.

REFERENCES

Specifier: If retaining this optional References Article, edit to include only those references cited in the edited section.

References, General: Versions of the following standards current as of the date of issue of the project apply to the Work of this Section.

ASTM International (ASTM): www.astm.org:

ASTM D638 – Standard Test Method for Tensile Properties of Plastics.

ASTM D2369- Standard Test Method for Volatile Content of Coatings

ASTM D3363- Standard Test Method for Film Hardness by Pencil Test

ASTM D-4060- Standard Test Method for Abrasion Resistance of Organic Coatings by the Taber Abraser

ASTM D1640- Standard Test Methods for Drying, Curing, or Film of Organic Coatings

ASTM D523- Standard Test for Specular Gloss

U. S. Environmental Protection Agency (EPA): www.epa.gov:

40 CFR 59, Subpart D - National Volatile Organic Compound Emission Standards for Architectural Coatings

ADMINISTRATIVE REQUIREMENTS

Preinstallation Conference: Conduct conference at Project Site.

Review requirements for flooring products and installation, including surface preparation, substrate conditions, expansion joints as required, project and manufacturer's details, installation procedures, mockups, testing and inspection requirements, protection and repairs, and coordination and sequencing of waterproofing work with work of other Sections.

ACTION SUBMITTALS

Product Data: For each type of flooring product (and expansion joint accessory if applicable) specified, including:

Technical data indicating compliance with requirements.

Substrate preparation instructions and recommendations.

Manufacturer’s Material Safety Data Sheet (SDS) for each product being used.

Shop Drawings: Show locations for flooring system components. Show details for each type of substrate, joints, corners, and edge conditions, including flashings, counterflashings, penetrations, transitions, and terminations.

INFORMATIONAL SUBMITTALS

Qualification Data: For Installer, manufacturer[, and flooring Inspector].

Certification of manufacturer's approval of Installer.

Low-Emitting Product Certificate: For flooring products specified to meet volatile organic emissions standards, submit Greenguard Children and Schools Certification or comparable certification acceptable to Architect.

Product Test Reports: Test data for flooring products and flooring system, by qualified testing agency, indicating proposed flooring meets performance requirements, when requested by Architect.

Warranty: Sample of unexecuted manufacturer and installer special warranties.

Field quality control reports.

QUALITY ASSURANCE

Installer Qualifications: The Applicator shall have been approved by the flooring system manufacturer in all phases of surface preparation and application of the specified system and have a minimum of 5 years relevant experience.

Manufacturer Qualifications: A qualified manufacturer [listed in this Section] with minimum seven years’ experience in manufacture of waterproofing as one of its principal products.

Manufacturer's product submitted has been in satisfactory operation on five similar installations for at least five years.

Specifier: Retain "Approval of Manufacturers and Comparable Products" Paragraph below to provide control over qualifying of substituted manufacturers.

Approval of Manufacturers and Comparable Products: [Submit] [Prime bidder must submit] the following in accordance with project substitution requirements, within time allowed for substitution review:

No requests for substitutions shall be considered that would change the generic type of the specified system.

System shall be in compliance with requirements of United States Department of Agriculture (USDA), Food Drug Administration (FDA), and local Health Department.

Completed and signed Substitution Request form.

Product data, including certified independent test data indicating compliance with requirements.

Sample shop drawings from similar project.

Project references: Minimum of five installations of similar system not less than five years old, with Owner and Architect contact information.

Name and resume of proposed qualified Inspector.

Sample warranty.

Specifier: Retain "Flooring Inspector Qualifications" Paragraph if Contractor is required to provide manufacturer inspections under Part 3 Field Quality Control article.

Flooring Inspector Qualifications: An independent party certified as a flooring inspector acceptable to Architect, retained by the Contractor and experienced in the installation and maintenance of the specified flooring system, qualified to perform observation and inspection specified in Field Quality Control Article, to determine Installer’s compliance with the requirements of this Project, and approved by the manufacturer to issue warranty certification.

Specifier: Retain "Testing Agency Qualifications" Paragraph if Contractor is required to provide independent inspections under Part 3 Field Quality Control article.

Testing Agency Qualifications: Qualified independent agency experienced in the installation of the specified flooring system, and qualified to perform observation and inspection specified in Field Quality Control Article to determine Installer’s compliance with the requirements of this Project, acceptable to Architect, retained by the Contractor.

Mockups: Provide flooring mockup application within mockups required in other sections, or if not specified, in an area of not less than 150 sq. ft. (14 sq. m) of surface where directed by Architect for each type of substrate condition. Include examples of surface preparation, crack and joint treatment, flooring application, and flashing, transition, and termination conditions, to set quality standards for execution.

If applicable, include no less than 13 ft (3.96m) including a minimum of one splice joint of Willseal® Expansion Joint System.

DELIVERY, STORAGE AND HANDLING

Accept materials on site in manufacturer's unopened original packaging, clearly identified with the product name and batch number.

Store products in weather protected environment, clear of ground and moisture, within temperature ranges recommended by flooring manufacturer.

      - The Applicator shall be provided with a dry storage area for all components. The area shall be between 50o F and 75o F, dry, out of direct sunlight and in accordance with the Manufacturer's recommendations and relevant health and safety regulations.

      - Copies of Material Safety Data Sheets (SDS) for all components shall be kept on site for review by the Engineer or other personnel.

Specifier: Retain first option in "Construction Waste" Paragraph below for LEED projects; retain second option for other projects.

Construction Waste: Store and dispose of packaging materials and construction waste in accordance with requirements of Division 01 Section ["Construction Waste Management"] ["Temporary Facilities and Controls."]

ENVIRONMENTAL REQUIREMENTS

Environmental Limitations: Apply flooring within the range of ambient and substrate temperatures recommended by flooring manufacturer.

Protect substrates from environmental conditions that affect flooring performance.

SCHEDULING

Coordinate installation of flooring with completion of other work requiring interface with flooring.

Schedule work so flooring applications may be inspected prior to concealment.

Ensure flooring materials are cured before covering with other materials.

WARRANTY

Specifier: Consult Tremco representative for available special project warranty terms and conditions.

Special Manufacturer's Warranty: Manufacturer's standard form in which flooring manufacturer agrees to furnish flooring material to repair or replace those materials installed according to manufacturer's written instructions that exhibit material defects or otherwise fail to perform as specified under normal use within warranty period specified.

Access for Repair: Owner shall provide unimpeded access to the Project and the flooring system for purposes of testing, leak investigation, and repair, and shall reinstall removed cladding and overburden materials upon completion of repair.

Cost Limitation: Manufacturer's obligation for repair or replacement shall be limited to the original installed cost of the work.

Warranty Period: [__] years date of Substantial Completion.

PRODUCTS

MANUFACTURERS

Specifier: Retain option for substitutions below and edit if required for project.

Basis-of-Design Products: Provide waterproofing products manufactured by Tremco, Inc., Commercial Sealants and Waterproofing Division, Beachwood OH; (866) 321-6357; email: techresources@tremcoinc.com; www.tremcosealants.com, [or comparable products of other manufacturer approved by Architect in accordance with Instructions to Bidders and Division 01 General Requirements]. If applicable, provide expansion joint products manufactured by Willseal, Hudson, NH; www.willseal.com .

Source Limitations: Provide flooring system materials and accessory products from single source from single manufacturer.

PERFORMANCE REQUIREMENTS

Compatibility: Provide flooring system materials that are compatible with one another and with adjacent materials under conditions of service and application required, as demonstrated by flooring manufacturer based on testing and field experience.

ARCHITECTURAL SOLID COATINGS: SEALERS

TREMCO Sealer 200: A high solids, two-component, UV-Stable Aliphatic Polyurethane topcoat.

1.  System Materials:

a.   Topcoat: TREMCO Sealer 200 Part A (0.65 gal), TREMCO Sealer Part B (0.35 gal).

B.        Product Requirements

Topcoat: TREMCO Sealer 200

1.  	Percent Solids: 78%

2. 	VOC, ASTM D2369: <5 g/L

3. 	Drying Time, 6 mils WFT, ASTM D 1640: 6 hours

4. 	Pencil Hardness, ASTM D3363: 2H

5. 	Taber Abrasion, CS 17 Wheel Impact, ASTM D 4060: Direct Impact >160-inch lbs., Indirect Impact > 160-inch lbs.

6.		Gloss 60°, ASTM D523: 85-90

EXECUTION

EXAMINATION

Surface Condition:  Examine substrates, areas and conditions, with Applicator present, for compliance with requirements for maximum moisture content, installation tolerances and other conditions affecting sealer performance.

Verify concrete and masonry surfaces are visibly dry, have cured for time period recommended by flooring manufacturer, and are free from release agents, curing agents, laitance, and other contaminates. Test for flooring adhesion per manufacturer's recommended method. Notify Architect of unsatisfactory conditions.

Proceed with installation only after unsatisfactory conditions have been corrected.

INTERFACE WITH OTHER WORK

Sequencing of Work:  Coordinate sequencing of flooring work with work of other sections that form portions of building envelope moisture control to ensure that expansion joints, flashings and transition materials can be properly installed and inspected.

Subsequent Work:  Coordinate flooring work with work of other sections installed subsequent to flooring to ensure complete inspection of installed flooring and sealing of flooring penetrations necessitated by subsequent work.

PREPARATION

General

All concrete surfaces shall be free of laitance, oil, grease, curing compounds, loose particles, friable matter, dirt, bituminous products, and all other contaminants.

Surface texture should be similar to 80- 100 grit sandpaper or the visual standard, CSP-1 from the International Concrete Repair Institute.

The prepared surface should have a nominal tensile strength of 250 psi per ASTM D-4541.

Additional surface preparation will be required if a 80-100-grit texture is not achieved and the surface laitance not completely removed after the first mechanical preparation procedure.

Moisture Testing: All concrete substrates must be checked for moisture prior to product application using the Plastic Sheet Test, ASTM D-4263.

FLOORING APPLICATION

General:

- The system shall be applied in two distinct steps

  - Substrate preparation

  - Topping application

- Immediately prior to the application of any component of the system, the surface shall be dry, and any remaining dust or loose particles shall be removed using a vacuum or clean, dry, oil- free compressed air.

- The handling, mixing and addition of components shall be performed in a safe manner to achieve the desired results in accordance with the Manufacturer's recommendations.

- A neat finish with well-defined boundaries and straight edges shall be provided by the applicator.

### B. 	Topcoat:

      - The topcoat shall be mixed and applied per manufacturer recommended procedure.

      - The topcoat shall be comprised of two components: TREMCO Sealer 200 Part A and TREMCO Sealer 200 Part B.

      - The mixing station shall be near the installation area. Using a slow-speed drill and jiffy blade, mix part A separately for approximately 1 minute before adding Part B.

      - Add the correct amount of Part B to Part A. Mix for 2-3 minutes to achieve a uniform consistency.

      - Apply at 250-300 sq ft at 6 mils WFT or 4-5 mils DFT. Coverage varies depending on aggregate size.

      - Back roll the applied Sealer 200 with a ¼” contractor grade nap mohair roller. Change the nap roller every 800 sq ft to avoid the activation of the resin in the roller.

      - Use a paint brush or mini roller to ensure boards, edges, and corners are sealed appropriately.

FIELD QUALITY CONTROL

Tests, Inspection

The following tests shall be conducted by the Applicator:

Temperature

1.  Air, substrate temperatures and, if applicable, dew point.

Coverage Rates

1. Application rate shall be monitored by checking quantity of material used against covered area.

Where applicable, inspect transitional material such as expansion joints, flashings, insulation are installed per manufacturers recommendations.

Retain "Testing Agency" Paragraph below if applicable to Project, and edit to identify party retaining independent agency to perform tests and inspections.

Testing Agency: [Owner will engage] [Engage] a qualified testing agency to inspect substrate conditions, surface preparation, flooring application and to furnish reports to Architect.

Coordination of Inspection: Cooperate with testing agency.  Allow access to work areas and staging.  Notify testing agency in writing of schedule for Work of this Section to allow sufficient time for testing and inspection.

Do not cover Work until testing and inspection is completed and accepted.

Reporting:  Forward written inspection reports to the Architect within 10 working days of the inspection and test being performed.

Correction of Work:  Correct deficient applications not passing tests and inspections, make necessary repairs, and retest as required to demonstrate compliance with requirements.

CLEANING AND PROTECTING

Cure flooring material in compliance with manufacturer’s directions, taking care to prevent their contamination during stages of application and prior to completion of the curing process.

Remove masking. Perform detail cleaning at floor termination, to leave cleanable surface for subsequent work of other sections.

Clean tools and equipment immediately after use with Xylene, acetone, or denatured alcohol.

END OF SECTION