Tremco, Inc. Commercial Sealants and Waterproofing

Section 07 13 00 SHEET APPLIED WATERPROOFING SYSTEM
TREMproof® Amphibia Waterproofing System Guide Specification

TREMproof Amphibia is a self-healing, self-sealing and self-repairing sheet waterproofing membrane.  This co-extruded, watertight membrane has three active layers – a watertight EPDM barrier, and active core with the ability to heal itself when penetrated, and an active barrier which seals the overlap and prevents lateral movement of water.  Also, a non-woven fabric layer promotes the mechanical adhesion of the membrane to the concrete.

Basic Uses

Designed for use on blindside or backfilled walls, or split slab and below slab on grade

Can be used on damp or green concrete

Can be used in conjunction with TREMDrain® Series Drainage Mats

This section is easily edited using several common commercial specification software tools.

We recommend you consult with your Tremco technical representative, who can be contacted through: Tremco, Inc., Commercial Sealants and Waterproofing Division, Beachwood OH; (866) 321-6357; email: techresources@tremcoinc.com; www.tremcosealants.com.

Tremco products appear in the following CSI MasterFormat guide specifications available from Tremco:

• Section 07 01 91 Joint Sealant Rehabilitation and Replacement

• Section 07 13 00 Sheet Applied Waterproofing (TREMproof Amphibia)

• Section 07 14 13.01 Hot Fluid-Applied Waterproofing, Deck (TREMproof 6100)

• Section 07 14 13.02 Hot Fluid-Applied Waterproofing, Vegetated Roof (TREMproof 6100)

• Section 07 14 16.01 Cold Fluid-Applied Waterproofing, Vertical and Deck (TREMproof 250GC)

• Section 07 14 16.02 Cold Fluid-Applied Waterproofing, Vertical (TREMproof 250GC)

• Section 07 14 16.03 Cold Fluid-Applied Waterproofing, Deck (TREMproof 250GC)

• Section 07 14 16.04 Cold Fluid-Applied Waterproofing, Vegetative Roof (TREMproof 250GC)

• Section 07 17 16.01 Dual HDPE/Bentonite Waterproofing System (Paraseal)

• Section 07 17 16.03 Dual HDPE/Bentonite Waterproofing System(Paraseal GM)

• Section 07 17 16.04 Dual HDPE/Bentonite Waterproofing System(Paraseal GM/LG 20-MIL)

• Section 07 17 16.05 Dual HDPE/Bentonite Waterproofing System(Paraseal GM/LG 60-MIL)

• Section 07 18 00.01 Traffic Coatings, Vehicular

• Section 07 18 00.02 Traffic Coatings, Pedestrian

• Section 07 18 00.03 Traffic Coatings, Mechanical Rooms

• Section 07 27 13 Modified Bituminous Sheet Air Barriers, Vapor-Retarding (ExoAir 110)

• Section 07 27 23 Board Product Air Barriers, Vapor Permeable (SECUREROCK ExoAir 430)

• Section 07 27 26.01 Fluid-Applied Membrane Air Barriers, Vapor-Retarding (ExoAir 120)

• Section 07 27 26.02 Fluid-Applied Membrane Air Barriers, Vapor Permeable (ExoAir 220)

• Section 07 27 26.03 Fluid-Applied Membrane Air Barriers, Vapor Permeable (ExoAir 230)

• Section 07 92 00 Joint Sealants

• Section 08 85 00 Glazing Sealants

• Section 32 13 73 Concrete Paving Joint Sealants

This document includes Specifier notes in hidden text. To view hidden text, www.bim.net/displaying-hidden-text-in-microsoft-word-step-by-step-instructions-for-windows-and-mac/

Paraseal®, TREMproof®, ExoAir®, Spectrem®, Tremflex®, Dymonic®, Dymeric®, and Proglaze® are registered trademarks of Tremco, Inc.

SECUREROCK® is a registered trademark of United States Gypsum Company. AMPHIBIA™ is a trademark of Volteco S.p.A.
This document is Copyright© 2014 by Tremco, Inc.

SECTION 07 13 00 – SHEET WATERPROOFING

- GENERAL

      - RELATED DOCUMENTS

        - Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this section.

      - SUMMARY

        - Section Includes:

          - Sheet Waterproofing

          - Molded sheet drainage panels

Specifier: If retaining this optional Related Requirements Article, edit to include only those sections included in project manual.

      - REFERENCE STANDARDS

Specifier: If retaining this optional References Article, edit to include only those references cited in the edited section.

        - References, General: Versions of the following standards current as of the date of issue of the project apply to the Work of this Section.

        - ASTM International (ASTM): www.astm.org:

          - ASTM C836 – Standard Test Methods for Crack Cycling

          - ASTM D412 - Standard Test Methods for Vulcanized Rubber and Thermoplastic Elastomers – Tension

          - ASTM D624 - Standard Test Method for Tear Strength of Conventional Vulcanized Rubber and Thermoplastic Elastomers

          - ASTM D903 - Standard Test Method for Peel or Stripping Strength of Adhesive Bonds

          - ASTM D3767 - Standard Practice for Rubber—Measurement of Dimensions

          - ASTM D1970 - Standard Specification for Self-Adhering Polymer Modified Bituminous Sheet Materials Used as Steep Roofing Underlayment for Ice Dam Protection

          - ASTM D4833 - Standard Test Method for Index Puncture Resistance of Geomembranes and Related Products

          - ASTM D5385/5385M - Standard Test Method for Hydrostatic Pressure Resistance of Waterproofing Membranes

          - ASTM E96/E 96M - Standard Test Methods for Water Vapor Transmission of Materials

          - ASTM D4068 - Standard Specification for Chlorinated Polyethylene (CPE) Sheeting for Concealed Water-Containment Membrane

          - ASTM D5385 - Standard Test Method for Hydrostatic Pressure Resistance of Waterproofing Membranes

          - ASTM D570 - Standard Test Method for Water Absorption of Plastics

        - U. S. Environmental Protection Agency (EPA): www.epa.gov.

      - ADMINISTRATIVE REQUIREMENTS

        - Preinstallation Conference: Conduct conference at Project Site.

          - Review requirements for waterproofing products and installation, including surface preparation, substrate conditions, project and manufacturer's details, installation procedures, mockups, testing and inspection requirements, protection and repairs, and coordination and sequencing of waterproofing installation with work of other Sections.

      - ACTION SUBMITTALS

        - Product Data: For each type of waterproofing product specified, including:

          - Include construction details, material descriptions, and tested physical and performance properties of waterproofing.

          - Include manufacturer's written instructions for evaluating, preparing, and treating substrate.

        - LEED Submittals:

          - Product Certificates for Credit MR 5:  For products and materials required to comply with requirements for regional materials, certificates indicating location of material manufacturer and point of extraction, harvest, or recovery for each raw material.  Include statement indicating distance to Project, cost for each regional material, and fraction by weight that is considered regional.

        - Shop Drawings: Show locations for waterproofing system components. Show details for each type of substrate, joints, corners, and edge conditions, including flashings, counter-flashings, penetrations, transitions, and terminations.

        - Samples:  For each exposed product and for each color and texture specified, including the following products:

          - 8-by-8-inch (200-by-200-mm) square of waterproofing and flashing sheet.

          - 4-by-4-inch (100-by-100-mm) square of drainage panel.

      - INFORMATIONAL SUBMITTALS

        - Qualification Data: For Installer.

        - Warranty: Sample of special warranties.

        - Field quality control reports.

      - QUALITY ASSURANCE

        - Installer Qualifications: An entity that employs installers and supervisors who are trained and approved by waterproofing manufacturer.

        - Mockups:   Build mockups to verify selections made under Sample submittals and to set quality standards for installation.

          - Build for each typical waterproofing installation including accessories to demonstrate surface preparation, crack and joint treatment, corner treatment, and protection.

            - Size:  As shown on Drawings.

            - Description:  Each type of wall installation.

          - Approval of mockups does not constitute approval of deviations from the Contract Documents contained in mockups unless Architect specifically approves such deviations in writing.

          - Subject to compliance with requirements, approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

      - FIELD CONDITIONS

        - Environmental Limitations:  Apply waterproofing within the range of ambient and substrate temperatures recommended by waterproofing manufacturer.

          - Do not apply waterproofing in snow, rain or fog.

        - Maintain adequate ventilation during preparation and application of waterproofing materials.

      - DELIVERY, STORAGE AND HANDLING

        - Accept materials on site in manufacturer's unopened original packaging.

        - Store products in weather protected environment, clear of ground and moisture, within temperature ranges recommended by waterproofing manufacturer.

Specifier: Retain first option in "Construction Waste" Paragraph below for LEED projects; retain second option for other projects.

        - Construction Waste: Store and dispose of packaging materials and construction waste in accordance with requirements of Division 01 Section ["Construction Waste Management"] ["Temporary Facilities and Controls."]

      - SCHEDULING

        - Schedule work so waterproofing applications may be inspected prior to concealment.

      - WARRANTY

        - Manufacturer's Warranty:  Manufacturer's standard materials-only warranty in which manufacturer agrees to furnish replacement waterproofing material for waterproofing that does not comply with requirements or that fails to remain watertight within specified warranty period.

          - Warranty Period:  ____ years from date of Substantial Completion.

        - Installer's Special Warranty:  Specified form, signed by Installer, covering Work of this Section, for warranty period of ___ years.

          - Warranty includes removing and reinstalling protection board and drainage panels,

- PRODUCTS

      - MATERIALS, GENERAL

        - Source Limitations: Provide waterproofing system materials and accessory products from a single-source system manufacturer.

      - PERFORMANCE REQUIREMENTS

        - General: Waterproofing system shall be capable of performing as a continuous watertight installation and as a moisture drainage plane transitioned to adjacent flashings and discharging water to the building exterior. Waterproofing shall accommodate normal substrate movement, construction material transitions, opening transitions, penetrations, and perimeter conditions without resultant moisture deterioration.

        - Compatibility: Provide waterproofing system materials that are compatible with adjacent materials under conditions of service and substrates on which product is applied, as recommended by waterproofing manufacturer based on testing and field experience.

      - SHEET WATERPROOFING

Specifier: Tremco's Paraseal includes an integral HDPE membrane protective facing.

Specifier: Tremco's Paraseal LG includes an integral HDPE membrane protective facing plus an additional protective laminate layer of spun polypropylene for use in horizontal and vertical applications over lagging on blindside walls, below-slab, and for shotcrete applications.

        - Multi-Layer Sheet Waterproofing: Composite membrane of 63 mils thickness consisting of an EPDM watertight barrier layer, a hydro-reactive polymer core layer, an EPDM derivative/polymer hydro-reactive layer, and a non-woven polyethylene geotextile facing.

          - Products:  Subject to compliance with requirements, provide the following:

            - Basis of Design Product: Tremco, Inc., TREMproof Amphibia

          - Physical Properties:

            - Elongation, ASTM D412:  709%

            - Tensile Strength, ASTM D 412: 927 psi

            - Nail Sealability, ASTM D1970, sect. 7.9: Passed

            - Low Temp Flexibility @ -20° F, ASTM D1970, sect. 7.6: Unaffected, passed

            - Peel Adhesion to Concrete, ASTM D903: 7.7 lbs./in.

            - Strength at Break, ASTM D624: 161.51 psi

            - Permeance, ASTM E96 B:0.069 US Perms, 0.016 US Perms (BW - Inverted Wet Cup)

            - Resistance to Hydrostatic Head, ASTM D5385: Pass at 231 ft.²

            - Thickness, ASTM D3767: 63 mils, 1.6mm

            - Crack Cycling @ -9.4° F, 100 cycles, ASTM C836:  Unaffected, Pass

            - Puncture Resistance of Geomembranes, ASTM D4833: 52.4 kg/M

            - Hydrostatic Pressure Resistance, ASTM D4068: Pass at 40 hrs.

            - Water Absorption, ASTM D570: 0.13%

            - Installation Temperatures: 32 to 95°F (0 to 35° C)

            - Freeze/Thaw Cycles:  no effect before or after installation

            - Life Expectency: Indefinite

            - Color: Black

Specifier: Tremco's Deckseal has transparent HDPE membrane protective facing for use on elevated horizontal surfaces where flood-testing is required; use with waterproof seam tape.

      - ACCESSORY MATERIALS

        - General:  Furnish accessory materials recommended by waterproofing manufacturer for intended use and compatible with sheet waterproofing.

        - Termination Bar: Extruded-aluminum or formed-stainless-steel bars with upper flange to receive sealant.

            - Basis of Design Product – Tremco, Inc., Paraterm Bar

        - Tapes: Waterproofing manufacturer's recommended tape for joints between sheets, membranes, or panels.

          - Safety Overlap Tape:  butyl-hybrid adhesive tape with a fleece face.

            - Basis of Design Product: Tremco, Inc. Tremco BG Grip Tape

        - Waterstops: hydro-reactive, water swelling, single component elastic sealant.

            - Basis of Design Product – Adeka ULTRASEAL P-201

        - Joint Sealants: Termination Seals:

          - Single component, high performance, medium-modulus, low-VOC, UV-stable, non-sag polyurethane sealant.

            - Basis of Design Product: Tremco Inc.; Dymonic 100.

Specifier: Select drainage panel from among eight types listed below in consultation with soils engineer based upon subsurface water conditions and application.

      - WATERPROOFING PROTECTION AND DRAINAGE PANELS

        - Protection Course: Not required.

Specifier: Tremco TREMDrain drainage panel is for general use at backfilled and blindside wall locations.

        - Nonwoven-Geotextile-Faced, Molded-Sheet Drainage Panel: Manufactured composite subsurface drainage panels consisting of a nonwoven, spun-bonded polypropylene facing laminated to one side of a studded, non-biodegradable, polystyrene drainage core.

          - Basis of Design: Tremco, TREMDrain.

          - Flow Capacity, per unit width, ASTM D 4716: 12.5 gpm/ft. (155 lpm/m).

          - Flow Rate, ASTM D 4491: 165 gpm/ft2 (6,724 lpm/m2).

          - Apparent Opening Size: No. 70 sieve (210 micron).

          - CBR Puncture, ASTM D 6241: 275 lb. (1,220 N).

          - Core Compressive Strength, ASTM D 1621: 11,000 lb/ft2 (527 kN/m2).

          - Thickness: 0.25 inch (6.35 mm).

Specifier: Tremco TREMDrain 1000 drainage panel is for use at backfilled and blindside wall and underslab locations requiring a higher compressive strength core or greater flow capacity. It is available with an optional polymeric film backer ( "PF").

        - Nonwoven-Geotextile-Faced, Molded-Sheet Drainage Panel: Manufactured composite subsurface drainage panels consisting of a nonwoven, spun-bonded polypropylene facing laminated to one side of a studded, non-biodegradable, polystyrene drainage core[, with polymeric film attached to back of drainage core].

          - Basis of Design: Tremco, TREMDrain [1000] [1000 PF].

          - Flow Capacity, per unit width, ASTM D 4716: 18 gpm/ft. (224 lpm/m).

          - Flow Rate, ASTM D 4491: 165 gpm/ft2 (6,724 lpm/m2).

          - Apparent Opening Size: No. 70 sieve (210 micron).

          - CBR Puncture, ASTM D 6241: 275 lb (1,220 N).

          - Core Compressive Strength, ASTM D 1621: 15,000 lb/ft2 (718 kN/m2).

          - Thickness: 0.437 inch (11 mm).

Specifier: Tremco TREMDrain 2000 three-layer drainage panel is for use at split slabs and planters requiring a higher compressive strength core or greater flow capacity. It includes a polymeric film backer.

        - Drainage Panel: Manufactured composite subsurface drainage panels consisting of a nonwoven, spun-bonded polypropylene facing laminated to one side of a studded, non-biodegradable, polystyrene drainage core, with polymeric film attached to back of drainage core.

          - Basis of Design: Tremco, TREMDrain 6000/6000PF.

          - Flow Capacity, per unit width, ASTM D 4716: 18 gpm/ft. (223 lpm/m).

          - Flow Rate, ASTM D 4491: 150 gpm/ft2 (6,113 lpm/m2).

          - Apparent Opening Size: 70 sieve (210 micron).

          - CBR Puncture, ASTM D 6241: 320 lb (1,410 N).

          - Core Compressive Strength, ASTM D 1621: 15,000 lb/ft2 (718 kN/m2).

          - Thickness: 0.40 inch (10 mm).

Specifier: Tremco TREMDrain GS 0.5 inch thick three-layer drainage panel is for use at planters. It includes a polymeric film backer; the core also functions as a water retention layer. GS mats are available with optional copper hydroxide-treated root control polymeric film to help control aggressive plant root structures.

Specifier: Tremco TREMDrain GS 1.0 inch thick three-layer drainage panel is for use at planters. It includes a polymeric film backer; the core also functions as a water retention layer. GS mats are available with optional copper hydroxide-treated root control polymeric film to help control aggressive plant root structures. Below has higher flow capacity than above.

Specifier: Tremco TREMDrain TotalDrain is a two-layer drainage panel with high-profile drainage section for water collection and flow around the structure plus a transition section to connect to other TREMDrain panels, for use on backfilled walls and blindside walls.

        - Nonwoven-Geotextile-Faced, Molded-Sheet Drainage Panel: Manufactured composite subsurface drainage panels consisting of a nonwoven, needle-punched polypropylene facing laminated to one side of a studded, non-biodegradable, polystyrene drainage core.

          - Basis of Design: Tremco, TREMDrain TotalDrain.

          - Flow Capacity, per unit width, ASTM D 4716: 21 @ HG= 0.1, 261@HG=0.1

          - Flow Rate, ASTM D 4491: 150 gpm/ft2 (6,113 lpm/m2).

          - Apparent Opening Size: 70 sieve (210 micron).

          - CBR Puncture, ASTM D 6241: 320 lb (1,410 N).

          - Core Compressive Strength, ASTM D 1621: 9,500 lb/ft2 (455 kN/m2).

          - Thickness: 0.437 inch (11 mm), 1 inch (25mm).

Specifier: Tremco TREMDrain TotalDrain High Profile is a two-layer drainage panel with high-profile drainage section for water collection and flow around the structure plus a transition section to connect to other TREMDrain panels, for use on backfilled walls and blindside walls. Below has higher flow capacity than above.

- EXECUTION

      - EXAMINATION

        - Surface Condition: Before applying waterproofing materials, examine substrate conditions.

        - Proceed with installation once unsatisfactory conditions have been corrected.

      - INTERFACE WITH OTHER WORK

        - Sequencing of Work: Coordinate sequencing of waterproofing installation with work of other sections that form portions of building envelope moisture control to ensure that flashings and transition materials can be properly installed and inspected.

        - Subsequent Work: Coordinate waterproofing installation with work of other sections installed subsequent to waterproofing to ensure complete inspection of installed waterproofing and sealing of waterproofing penetrations necessitated by subsequent work.

      - PREPARATION

        - Clean, prepare, and treat substrates. Fill voids with cement grout as recommended by manufacturer.

        - Formed Concrete Surfaces: Remove fins and projections. Fill voids, form-tie holes, and other defects greater than 1/4 inch (6 mm) in depth.

        - Horizontal Concrete Surfaces: Remove standing water, debris, and substances that may impair bonding of patching materials or effectiveness of waterproofing. Fill voids and other defects greater than 1/4 inch (6 mm) in depth.

        - Excavation Support and Protection System: Fill minor gaps and spaces 1 (25 mm) wide or wider with appropriate filling material. Cover or fill large voids and crevices.

      - INSTALLATION, GENERAL

        - Install waterproofing and accessories according to manufacturer's written instructions.

          - Install a continuous layer of waterproofing membrane with ends and edges lapped a minimum of 2-4 inches (102 mm). Stagger end joints, seal laps and treat fastener penetrations in accordance with manufacturer’s written instructions.

          - Apply hydro-reactive expandable sealant around penetrations in horizontal and vertical surfaces, construction joints in substrate, and penetrations.

          - Apply Tremco 830 sealant between all overlaps and compress with a 2” x 2” steel seam roller using pressure sufficient to adequately flatten/spread the sealant bead.

          - Seal all overlaps with Tremco BG Grip Tape centered on the adjacent sheet edge, adhering to the white, non-woven fleece fabric layer facing the installer and pressing or rolling down to ensure full adhesion.

        - Protect waterproofing from damage during construction. Repair punctures, tears, and cuts.

Specifier: Retain installation articles and paragraphs that correspond to Project scope of work; delete all others.

      - VERTICAL BLINDSIDE WALL WATERPROOFING

        - Install Amphibia membrane with the white, fleece fabric side to be in direct contact with concrete and over a continuous layer of a TREMDrain drainage board. TREMDrain drainage board is applied 4 feet (1.2 m) above submerged conditions.

        - On shoring walls, install membrane with a minimum 2 – 4 inches (101.6 mm) sheet edge overlaps.  Tack membrane to highest point of shoring.  All overlaps of Amphibia must be treated in accordance with manufacturer’s details.

        - Verify which penetrations must be accessed after concrete placement for completion of waterproofing detail treatment and ensure that sufficient access to membrane is provided within a wood formed box out; verify which penetrations will not be accessed after concrete placement for completion of waterproofing detail treatment and ensure that final detailing procedures are completed prior to concrete pour; waterproof penetrations in accord with manufacturer’s current procedures; contact manufacturer for procedures at  project conditions not provided in installation manuals.

        - After any precipitation, pump standing water off waterproofing as soon as possible and repair any damage to membrane.

        - Excavation Support and Protection: Cut, clean, and treat tiebacks and similar projections. Encase tieback rods, nuts, and plates. If water is present, cover shoring and lagging with plastic protection sheets. If water is present, set up a dewatering system to remove water.

      - HORIZONTAL WATERPROOFING

        - Horizontal Roofs, Plazas, and between Slabs: Install waterproofing membrane starting at lowest point, with ends and edges overlapped a minimum of 2 - 4 inches (102 mm) and tape sealed.

          - Install fleece fabric side of membrane against the material to be waterproofed.

          - Terminations at Vertical Surfaces: Provide a fillet or cant at intersection of horizontal and vertical substrates.

      - BELOW-SLAB WATERPROOFING

        - Below Structural Slabs-on-Grade: Apply waterproofing membrane with black EPDM side down, and white, fleece fabric side up.

          - Install membrane sheets with the fleece fabric side up. Tape all seams where subject to displacement during concrete placement.

          - Install under footings, grade beams, and pile caps; or continue waterproofing through key joints between footings and foundation walls, and extend a minimum of 8 inches (200 mm) up or beyond perimeter slab forms. Stagger seams minimum 12 inches (305 mm).

          - Install under slabs starting at lowest point, install a continuous layer of waterproofing membrane, with ends and edges lapped a minimum of 4 inches (102 mm).

          - Protect waterproofing from damage caused by reinforcing bar supports with sharp edges.

      - DRAINAGE PANEL INSTALLATION

        - Place and secure drainage panels in accordance with manufacturer’s written instructions. Use adhesives that do not penetrate waterproofing. Lap edges and ends of geotextile to maintain continuity. Protect installed molded-sheet drainage panels during subsequent construction.

Retain subparagraph below if board insulation is installed before installing molded-sheet drainage panels.

        - Insulation: Refer to Section 07 20 00 "Thermal Insulation."

      - FIELD QUALITY CONTROL

        - Testing Agency: [Owner will] [Contractor shall] engage a qualified testing agency to inspect substrate conditions, surface preparation, waterproofing application, protection, and drainage components, and to furnish reports to Architect.

Retain one of two of the following testing Paragraphs.

Retain "Flood Testing" Paragraph below for elevated horizontal concrete slabs with HDPE membrane installed on top of waterproof membrane. Seams should be taped or otherwise sealed according to manufacturer's written instructions prior to flood testing.

        - Reporting: Forward written inspection reports to the Architect of the inspection and test being performed.

        - Correction: Correct deficient applications not passing tests and inspections, make necessary repairs, and retest as required to demonstrate compliance with requirements.

      - CLEANING AND PROTECTING

        - Protect Amphibia membrane from damage prior to concrete placement.

- END OF SECTION