Tremco, Inc. Commercial Sealants and Waterproofing

Section 07 14 16 COLD FLUID-APPLIED WATERPROOFING
Vertical Applications

Specifier: This guide specification section specifies Tremco TREMproof® 260 cold fluid-applied waterproofing. TREMproof 260 is a polymer-enhanced, single component, fluid-applied, asphalt emulsion, below-grade waterproofing membrane.  It is available in both a spray and roller grade.

• Designed for use on backfilled walls, Nudura Insulated Concrete Forms (ICF), Insulated concrete forms, and blindside walls with carrier sheets.

Separate guide specification sections are available from Tremco for vertical, horizontal (deck), and vegetative roof applications. This section is easily edited using several common commercial specification software tools.

We recommend you consult with your Tremco technical representative, who can be contacted through: Tremco, Inc., Commercial Sealants and Waterproofing Division, Beachwood OH; (866) 321-6357); email: techresources@tremcoinc.com;  www.tremcosealants.com.

Tremco sealant and waterproofing products appear in the following CSI MasterFormat specifications sections:

• Section 07 01 91 Joint Sealant Rehabilitation and Replacement
• Section 07 14 13.01 Hot Fluid-Applied Waterproofing, Deck (TREMproof 6100)
• Section 07 14 16.02 Cold Fluid-Applied Waterproofing, Vertical (TREMproof 250GC)

• Section 07 14 16.03 Cold Fluid-Applied Waterproofing, Vertical (TREMproof 260)
• Section 07 14 16.04 Cold Fluid-Applied Waterproofing, Vegetative Roof (TREMproof 250GC)

• Section 07 14 16.05 Cold Fluid-Applied Waterproofing, Vertical (TREMproof 201-60)
• Section 07 17 00 Bentonite Waterproofing (Paraseal GM/LG 60 mil)
• Section 07 18 00.01 Traffic Coatings, Vehicular
• Section 07 18 00.02 Traffic Coatings, Pedestrian
• Section 07 18 00.03 Traffic Coatings, Vehicular and Pedestrian
• Section 07 27 13 Modified Bituminous Sheet Waterproofing, Vapor-Retarding (ExoAir 110)
• Section 07 27 23 Board Product Waterproofing, Vapor Permeable (SECUREROCK ExoAir 430)
• Section 07 27 26.01 Fluid-Applied Membrane Waterproofing, Vapor-Retarding (ExoAir 120)
• Section 07 27 26.02 Fluid-Applied Membrane Waterproofing, Vapor Permeable (ExoAir 220)
• Section 07 27 26.03 Fluid-Applied Membrane Waterproofing, Vapor Permeable (ExoAir 230)
• Section 07 84 13 Penetration Firestopping
• Section 07 84 46 Fire-Resistive Joint Systems
• Section 07 92 00 Joint Sealants
• Section 08 85 00 Glazing Sealants
• Section 32 13 73 Concrete Paving Joint Sealants

TREMproof®, ExoAir®, Spectrem®, Tremflex®, Dymeric®, and Proglaze® are registered trademarks of Tremco, Inc.
This document is Copyright© 2014 by Tremco, Inc.

SECTION 07 14 16 – COLD FLUID-APPLIED WATERPROOFING

- GENERAL

      - SUMMARY

        - Section Includes:

          - Cold fluid-applied waterproofing, vertical.

          - [Protection course] [Drainage panels] [Insulation] [Insulation drainage panels].

      - RELATED REQUIREMENTS

Specifier: If retaining this optional Related Requirements Article, edit to include only those sections included in project manual.

          - Section 03 31 00 "Cast-in-Place Concrete" for moisture curing of concrete waterproofing substrate.

          - Section 04 20 00 "Unit Masonry" for compatibility with flashing components.

          - Division 07 air barrier section for wall waterproofing and interface coordination.

          - Section 07 72 73 "Membrane Leak Detection System" for requirements for EFVM leak detection system installation and membrane leak testing.

          - Section 07 76 13 "Roof Pavers" for requirements for roof ballast and roof decking pavers and support pedestal systems.

          - Section 07 92 00 "Joint Sealants" for joint sealants and accessories and joint preparation.

          - Section 07 90 00/07 95 00 "Expansion Control/Protection" for expansion joint systems.

          - Section 32 97 00 "Vegetated Roof Assemblies" for growing media, plantings, filter fabrics, root barriers, and related components.

          - Section 33 46 00 "Subdrainage" for drainage pipe and conduits, drainage panels, and filter fabrics.

      - REFERENCES

Specifier: If retaining this optional References Article, edit to include only those references cited in the edited section.

        - References, General: Versions of the following standards current as of the date of issue of the project apply to the Work of this Section.

        - ASTM International (ASTM): www.astm.org:

          - ASTM C 836 – Standard Specification for High-Solids Content, Cold Liquid-Applied Elastomeric Waterproofing Membrane for Use with Separate Wearing Course

          - ASTM D903 - Standard Test Method for Peel or Stripping Strength of Adhesive Bonds

          - ASTM D412 – Standard Test Methods for Vulcanized Rubber and Thermoplastic Elastomers – Tension

          - ASTM E96/E96M – Standard Test Methods for Water Vapor Transmission of Materials

        - U. S. Environmental Protection Agency (EPA): www.epa.gov:

          - 40 CFR 59, Subpart D - National Volatile Organic Compound Emission Standards for Architectural Coatings

      - ADMINISTRATIVE REQUIREMENTS

        - Preinstallation Conference: Conduct conference at Project Site.

          - Review requirements for waterproofing products and installation, including surface preparation, substrate conditions, expansion joints as required, project and manufacturer's details, installation procedures, mockups, testing and inspection requirements, protection and repairs, and coordination and sequencing of waterproofing work with work of other Sections.

      - ACTION SUBMITTALS

        - Product Data: For each type of waterproofing product (and expansion joint accessory if applicable) specified, including:

          - Technical data indicating compliance with requirements.

          - Substrate preparation instructions and recommendations.

        - Shop Drawings: Show locations for waterproofing system components. Show details for each type of substrate, joints, corners, and edge conditions, including flashings, counterflashings, penetrations, transitions, and terminations.

      - INFORMATIONAL SUBMITTALS

        - Qualification Data: For Installer, manufacturer[, and waterproofing Inspector].

          - Certification of manufacturer's approval of Installer.

        - Low-Emitting Product Certificate: For waterproofing products specified to meet volatile organic emissions standards, submit Greenguard Children and Schools Certification or comparable certification acceptable to Architect.

        - Product Test Reports: Test data for waterproofing products and waterproofing system, by qualified testing agency, indicating proposed waterproofing meets performance requirements, when requested by Architect.

        - Warranty: Sample of unexecuted manufacturer and installer special warranties.

        - Field quality control reports.

      - QUALITY ASSURANCE

        - Installer Qualifications: A manufacturer-approved firm with minimum [three] years experience in installation of specified products in successful use on similar projects, employing workers trained by manufacturer, including a full-time on-site supervisor with a minimum of [three] years experience installing similar work, and able to communicate verbally with Contractor[, Architect,] and employees.

        - Manufacturer Qualifications: A qualified manufacturer [listed in this Section] with minimum five years experience in manufacture of waterproofing as one of its principal products.

          - Manufacturer's product submitted has been in satisfactory operation on five similar installations for at least five years.

Specifier: Retain "Approval of Manufacturers and Comparable Products" Paragraph below to provide control over qualifying of substituted manufacturers.

          - Approval of Manufacturers and Comparable Products: [Submit] [Prime bidder must submit] the following in accordance with project substitution requirements, within time allowed for substitution review:

            - Completed and signed Substitution Request form.

            - Product data, including certified independent test data indicating compliance with requirements.

            - Sample shop drawings from similar project.

            - Project references: Minimum of five installations of similar system not less than five years old, with Owner and Architect contact information.

            - Name and resume of proposed qualified Inspector.

            - Sample warranty.

Specifier: Retain "Testing Agency Qualifications" Paragraph if Contractor is required to provide independent inspections under Part 3 Field Quality Control article.

        - Testing Agency Qualifications: Qualified independent agency experienced in the installation of the specified waterproofing system, and qualified to perform observation and inspection specified in Field Quality Control Article to determine Installer’s compliance with the requirements of this Project, acceptable to Architect, retained by the Contractor.

        - Mockups: Provide waterproofing mockup application within mockups required in other sections, or if not specified, in an area of not less than 150 sq. ft. (14 sq. m) of surface where directed by Architect for each type of substrate condition. Include examples of surface preparation, crack and joint treatment, waterproofing application, and flashing, transition, and termination conditions, to set quality standards for execution.

          - Include intersection of deck waterproofing with adjacent vertical waterproofing and moisture control system.

          - If applicable,  include no less than 13 ft (3.96m) including a minimum of one splice joint of Willseal® Expansion Joint System.

      - DELIVERY, STORAGE AND HANDLING

        - Accept materials on site in manufacturer's unopened original packaging.

        - Store products in weather protected environment, clear of ground and moisture, within temperature ranges recommended by waterproofing manufacturer.

Specifier: Retain first option in "Construction Waste" Paragraph below for LEED projects; retain second option for other projects.

        - Construction Waste: Store and dispose of packaging materials and construction waste in accordance with requirements of Division 01 Section ["Construction Waste Management"] ["Temporary Facilities and Controls."]

      - ENVIRONMENTAL REQUIREMENTS

        - Environmental Limitations: Apply waterproofing within the range of ambient and substrate temperatures recommended by waterproofing manufacturer.

          - Protect substrates from environmental conditions that affect waterproofing performance.

          - Do not apply waterproofing during snow, rain, fog, or mist.

      - SCHEDULING

        - Coordinate installation of waterproofing with completion of roofing and other work requiring interface with waterproofing.

        - Schedule work so waterproofing applications may be inspected prior to concealment.

        - Ensure waterproofing materials are cured before covering with other materials.

      - WARRANTY

Specifier: Consult Tremco representative for available special project warranty terms and conditions.

        - Special Manufacturer's Warranty: Manufacturer's standard form in which waterproofing manufacturer agrees to furnish waterproofing material to repair or replace those materials installed according to manufacturer's written instructions that exhibit material defects or otherwise fail to perform as specified under normal use within warranty period specified.

          - Access for Repair: Owner shall provide unimpeded access to the Project and the waterproofing system for purposes of testing, leak investigation, and repair, and shall reinstall removed cladding and overburden materials upon completion of repair.

          - Cost Limitation: Manufacturer's obligation for repair or replacement shall be limited to the original installed cost of the work.

          - Warranty Period: [__] years date of Substantial Completion.

- PRODUCTS

      - MANUFACTURERS

Specifier: Retain option for substitutions below and edit if required for project.

        - Basis-of-Design Products: Provide waterproofing products manufactured by Tremco, Inc., Commercial Sealants and Waterproofing Division, Beachwood OH; (866) 321-6357; email: techresources@tremcoinc.com; www.tremcosealants.com, [or comparable products of other manufacturer approved by Architect in accordance with Instructions to Bidders and Division 01 General Requirements]. If applicable, provide expansion joint products manufactured by Willseal, Hudson, NH; www.willseal.com .

        - Source Limitations: Provide waterproofing system materials and accessory products from single source from single manufacturer.

      - PERFORMANCE REQUIREMENTS

        - General: Waterproofing system shall be capable of performing as a continuous watertight installation and as a moisture drainage plane transitioned to adjacent flashings and discharging water to the building exterior. Waterproofing shall accommodate normal substrate movement and seal expansion and control joints, construction material transitions, opening transitions, penetrations, and perimeter conditions without resultant moisture deterioration.

Specifier: Paragraph below may apply to limitations on VOCs of authorities having jurisdiction; verify local requirements.

        - VOC Content: 72 g/L maximum per 40 CFR 59, Subpart D (EPA Method 24) and complying with requirements of authorities having jurisdiction.

        - Compatibility: Provide waterproofing system materials that are compatible with one another and with adjacent materials under conditions of service and application required, as demonstrated by waterproofing manufacturer based on testing and field experience.

      - WATERPROOFING MEMBRANE

        - Cold Fluid-Applied Waterproofing: polymer-enhanced, single component, fluid-applied, asphalt emulsion, below-grade waterproofing membrane.

          - Basis of Design Product: Tremco, Inc., TREMproof 260.

          - VOC Content:  No more than 72 g/L

          - Hardness, ASTM D 2240: 50 minimum; Pass.

          - Low Temperature Crack Bridging, ASTM C836; Modified ASTM C1305: Pass.

          - Adhesion-in-Peel after Water Immersion, ASTM C836; ASTM C794: Exceeds

          - Elongation, ASTM D412: 800%

          - Peel adhesion, ASTM D903: Passes

          - Low-Temp Flexibility, ASTM C836: Pass

          - Water resistance, ASTM C836, AATC-127: Pass

          - Water Vapor Permeance E96 Dry Cup: 0.028 US Perms

          - Water Vapor Permeance E96 Wet Cup: 0.032 US Perms

          - Stability (80°F/26.7°C): 6 months Minimum 1 year

          - Solids 64%, Density 8.1 lb/gal

      - ACCESSORY MATERIALS

        - General: Accessory materials as described in manufacturer's written installation instructions, recommended to produce complete waterproofing system meeting performance requirements, and compatible with waterproofing material and adjacent materials.

        - Elastomeric Detail Sheet: Blended thermoset elastomeric sheet reinforced with polyester woven scrim.

          - Basis of Design Product: Tremco, TRA Elastomeric Sheeting.

        - Elastomeric transition flashing to above-grade: polyurethane liquid-applied coating system with ultraviolet protective topcoat.

          - Basis of Design Product: Vulkem 350/351; Tremco Inc.

          - Basis of Design Product: Vulkem 801; Tremco Inc.

        - Metal Termination Bars: Waterproofing manufacturer's standard aluminum or stainless steel termination bar, with stainless steel fasteners.

        - Joint Sealant: ASTM C 719, high performance, medium-modulus, low-VOC, UV-stable, non-sag polyurethane sealant approved by waterproofing manufacturer for adhesion and compatibility with waterproofing and accessories.

          - Basis of Design Product: Tremco, Dymonic 100.

        - Basis of Design Product: Tremco, TREMproof 260.

        - Expansion Joint Pre-compressed or Closed Cell, Monolithic Foam System. Foam Structure Must not Contain Unbonded Foam Laminations;

          - Willseal® Coreseal for use in both vertical and horizontal below grade system applications requiring +/-25% movement capability, closed cell, and a lightweight seal.

          - Willseal® Color Coreseal for use in both vertical and horizontal below grade system applications requiring +/-25% movement capability, closed cell, and a lightweight seal.

          - Willseal® Color Coreseal – CM for use in both vertical and horizontal below grade Tremco system applications requiring +/-25% movement capability, closed cell, and a lightweight seal with an integrated waterproofing membrane.

          - Willseal® 250 BG for use in below grade applications, requiring +/- 50% movement capability

      - PROTECTION COURSE

        - Protection Course: [Waterproofing manufacturer's standard protection course material recommended for application.] [Provide the following:]

Specifier: If stipulating type of protection course, retain second option in "Protection Course" Paragraph above and retain one or more of following protection course products based upon Project requirements. If more than one protection course is retained, add description of location or indicate location of each on Drawings.

Select polyethylene sheet thickness below based upon Project requirements. 20 mils thickness provides basic waterproofing and vapor barrier protection; 40 mils thickness also provides root barrier; 60 mils thickness provides protection against methane gas infiltration.

          - Polyethylene (PE) sheet, [20 mil (0.51 mm)] [40 mil (1.02 mm)] thick.

            - Basis of Design Product: Tremco, Polyethylene Protection/Root Barrier Course.

          - Extruded hollow-core copolymer mat.

            - Basis of Design Product: Tremco, 2450.

          - UV-resistant lightweight polyester mat.

            - Basis of Design Product: Tremco, Protection Mat.

          - Elastomeric Sheet: Blended thermoset elastomeric sheet reinforced with polyester woven scrim.

            - Basis of Design Product: Tremco, TRA Elastomeric Sheeting.

      - DRAINAGE PANELS

        - Drainage Mat: Composite mat with drainage core, filter fabric, and protective polymeric film[, recommended by waterproofing manufacturer for application.] [. Provide the following:]

Specifier: Tremco TREMDrain DPI is a drainage, protection and insulation board designed for use with TREMproof 260 spray-applied waterproofing membrane. Its glass fiber design promotes efficient water drainage and the retention of the board’s R-value.  The semi-rigid nature of the board acts as a protection course for the TREMproof 260 waterproofing membrane.

          - Unfaced Rigid Fiberglass Drainage Board: Dense fiberglass foundation and drainage board, with glass fibers oriented in laminar layers parallel to the plane of the board.

            - Basis of Design: Tremco, TREMDrain DPI.

            - Flow Capacity, per unit width, ASTM D 4716: 21 gpm/ft. (261 Lpm/M).

            - Drainage ability (Hydraulic gradient of 1.0) Gallons/Hour/Lineal Foot: 118

            - Thermal Resistance: R-5.0

            - Board size:  4’ x 4’

            - Board Thickness: 1-3/16”.

Specifier: Tremco TREMDrain 1000 two-layer drainage panel recommended for applications requiring moderate compression and flow capacity.  TREMDrain 1000PF includes a polymeric film attached to the back of the drainage core.

          - Nonwoven-Geotextile-Faced, Molded-Sheet Drainage Panel: Manufactured composite subsurface drainage panels consisting of a nonwoven, spun-bonded polypropylene facing laminated to one side of a studded, non-biodegradable, polystyrene drainage core [with polymeric film attached to back of drainage core].

            - Basis of Design: Tremco, TREMDrain 1000/1000PF.

            - Flow Capacity, per unit width, ASTM D 4716: 18 gpm/ft. (224 lpm/m).

            - Flow Rate, ASTM D 4491: 165 gpm/ft2 (6,724 lpm/m2).

            - Apparent Opening Size: No. 70 sieve (210 micron).

            - CBR Puncture, ASTM D 6241: 275 lb (1,220 N).

            - Core Compressive Strength, ASTM D 1621: 15,000 lb/ft2 (718 kN/m2).

            - Thickness: 0.4375 inch (11 mm).

Specifier: Tremco TREMDrain TotalDrain drainage panel has a unique polymeric core designed to transition water collected from any TREMDrain drainage product into a high-flow collection system.  It is for use on backfilled walls and is equipped to handle the water volume generated by TREMDrain sheet drains more effectively than a perforated pipe collection system.

          - Nonwoven-Geotextile-Faced, Molded-Sheet Drainage Panel: Manufactured composite subsurface drainage panels consisting of a nonwoven, needle-punched polypropylene facing laminated to one side of a studded, non-biodegradable, polystyrene drainage core.

            - Basis of Design: Tremco, TREMDrain TotalDrain.

            - Flow Capacity, per unit width, ASTM D 4716: 18 gpm/ft. (224 lpm/m).

            - Flow Rate, ASTM D 4491: 150 gpm/ft2 (6,113 lpm/m2).

            - Apparent Opening Size: No. 70 sieve (210 micron).

            - CBR Puncture, ASTM D 6241: 320 lb (1410 N).

            - Core Compressive Strength, ASTM D 1621: 9,500 lb/ft2 (455 kN/m2).

            - Thickness: 0.437 inch (11 mm).

      - INSULATION

Specifier: Retain "Insulation, General" Paragraph below if specifying insulation in another Section.

        - Insulation, General: Comply with Section 07 21 00 "Thermal Insulation."

Specifier: Retain "Board Insulation" Paragraph below if board insulation is required over waterproofing and is not specified in another Section. If not indicated on Drawings, insert thickness requirement.

        - Board Insulation: Extruded-polystyrene board insulation according to ASTM C 578, square or shiplap edged.

Specifier: Type IV and Type VI insulations in first two subparagraphs below are usually limited to vertical applications. Type VII and Type V insulations, with higher compressive strengths, are used on plaza decks.

          - Type VI, 40-psi (276-kPa) minimum compressive strength.

          - Type VII, 60-psi (414-kPa) minimum compressive strength.

          - Type V, 100-psi (690-kPa) minimum compressive strength.

      - INSULATION DRAINAGE PANELS

Retain "Unfaced, Wall-Insulation Drainage Panels" paragraph below if required for foundation-wall applications.

        - Unfaced, Wall-Insulation Drainage Panels: Extruded-polystyrene board insulation, ASTM C 578, Type VI, 40-psi (276-kPa) minimum compressive strength; unfaced; with shiplap or channel edges and with one side having grooved drainage channels.

Retain "Geotextile-Faced, Wall-Insulation Drainage Panels" paragraph below if required for foundation-wall applications.

        - Geotextile-Faced, Wall-Insulation Drainage Panels: Extruded-polystyrene board insulation, ASTM C 578, Type VI, 40-psi (276-kPa) minimum compressive strength; with tongue-and-groove edges and with one side having grooved drainage channels faced with a nonwoven-geotextile filter fabric.

Retain "Unfaced, Plaza-Deck, Insulation Drainage Panels" paragraph below if required for horizontal use.

        - Unfaced, Plaza-Deck, Insulation Drainage Panels: Extruded-polystyrene board insulation, ASTM C 578, Type VII, 60-psi (414-kPa) minimum compressive strength; unfaced; with shiplapped or channel edges and with one side having ribbed drainage channels.

Retain "Geotextile-Faced, Plaza-Deck, Insulation Drainage Panels" Paragraph below if required for horizontal use.

        - Geotextile-Faced, Plaza-Deck, Insulation Drainage Panels: Extruded-polystyrene board insulation, ASTM C 578, Type VII, 60-psi (414-kPa) minimum compressive strength; with tongue-and-groove edges, with one side having grooved drainage channels, and faced with manufacturer's standard, nonwoven-geotextile filter fabric.

- EXECUTION

      - EXAMINATION

        - Surface Condition:  Before applying waterproofing materials and accessories, examine substrate and conditions to ensure substrates are fully cured, smooth, clean, dry, and free from high spots, depressions, loose and foreign particles and other deterrents to adhesion, and conditions comply with manufacturer's written recommendations.

          - Verify concrete and masonry surfaces are free from release agents, curing agents, laitance, and other contaminates. Test for waterproofing adhesion per manufacturer's recommended method. Notify Architect of unsatisfactory conditions.

          - Verify masonry joints are filled with mortar and struck flush.

        - Proceed with installation only after unsatisfactory conditions have been corrected.

      - INTERFACE WITH OTHER WORK

        - Sequencing of Work:  Coordinate sequencing of waterproofing work with work of other sections that form portions of building envelope moisture control to ensure that expansion joints, flashings and transition materials can be properly installed and inspected.

        - Subsequent Work:  Coordinate waterproofing work with work of other sections installed subsequent to waterproofing to ensure complete inspection of installed waterproofing and sealing of waterproofing penetrations necessitated by subsequent work.

      - PREPARATION

        - Clean, prepare, and treat substrates in accordance with waterproofing manufacturer's written instructions.

          - Mask adjacent finished surfaces.

          - Remove contaminants and film-forming coatings from substrates.

          - Remove projections and excess materials and fill voids with substrate patching material.

          - Prepare and treat joints and cracks in substrate per ASTM D 4258 and waterproofing manufacturer's written instructions.

          - For accessory materials, follow manufacturers application instructions.

        - Detail Preparation: Prepare non-moving shrinkage cracks, large cracks, construction joints, expansion joints, projections and protrusions, penetrations, drains, and changes in plane in accordance with waterproofing manufacturer's written instructions and details, using accessory materials specified. The following are two acceptable options for detail preparation:

          - Adhere strips of elastomeric sheet to moving expansion joints on both sides in conjunction with a metal termination bar embedded in a layer of cold fluid-applied waterproofing and overlay with coat of cold fluid-applied waterproofing.

          - Apply single-component urethane within moving expansion joints and overlay with a coat of cold fluid-applied waterproofing.

        - Transitions to Adjacent Materials: Apply Tremco Approved Primer to transition cold fluid-applied waterproofing membrane to adjacent components of the building envelope.

      - WATERPROOFING INSTALLATION

        - General: Apply waterproofing material to form a seal to achieve a continuous waterproofing according to waterproofing manufacturer's written instructions. Apply waterproofing material within manufacturer's recommended application temperature ranges.

        - Cold Fluid-Applied Waterproofing: Apply waterproofing in total wet film thickness and with methods recommended in writing by waterproofing manufacturer.

        - Terminations: Install terminations of waterproofing membrane in accordance with ASTM C 898 Standard Guide for Use of High Solids Content, Cold Liquid-Applied Elastomeric Waterproofing Membrane with Separate Wearing Course and ASTM C 1471 Standard Guide for Use of High Solids Content Cold Liquid-Applied Elastomeric Waterproofing Membrane on Vertical Surfaces, as applicable to application, at not less than minimum height recommended by waterproofing manufacturer.

        - Coordination of Testing:

          - Coordinate application of waterproofing membrane with installation of membrane leak detection system specified in Section 07 72 73 "Membrane Leak Detection System."

          - Do not cover waterproofing until it has been tested and inspected by Owner's testing agency.

        - Correct deficiencies in or remove waterproofing that does not comply with requirements; repair substrates and reapply waterproofing components.

      - PROTECTION INSTALLATION

Specifier: Retain "Protection Course" or "Drainage Panel" Paragraph as applicable to Project. Coordinate with related work in Section 32 97 00 "Vegetated Roof Assemblies" and Section 33 46 00 "Subdrainage" where applicable.

        - Protection Course: Cover waterproofing with protection course following curing of waterproofing and prior to backfilling. Overlap protection course joints.

        - Drainage Panel: Place and secure drainage panels using methods that do not penetrate waterproofing. Lap edges or abut ends of geotextile.

        - Insulation: Install one or more layers of board insulation as required, staggering joints. Fit within 1/2 inch (12 mm) of projections and penetrations.

      - FIELD QUALITY CONTROL

        - Contractor's Inspector:  Contractor shall engage manufacturer's qualified Inspector full-time during the Work to perform tests and inspections, including documenting of waterproofing prior to concealment.

          - Contractor's Inspector shall measure membrane thickness with a wet film gauge during the application process at least once for every 100 sq. ft. (10 sq. m).

          - Provide written report of tests and inspections.

          - Where applicable, inspect transitional material such as expansion joints, flashings, insulation are installed per manufacturers recommendations.

        - Testing Agency: Owner will engage a qualified testing agency to perform tests and inspections.

Retain "Testing Agency" Paragraph below if applicable to Project, and edit to identify party retaining independent agency to perform tests and inspections.

        - Testing Agency: [Owner will engage] [Engage] a qualified testing agency to inspect substrate conditions, surface preparation, waterproofing application, protection, and drainage components, and to furnish reports to Architect.

          - Testing includes EFVM inspection prior to concealing deck waterproof membrane as specified in Section 07 72 73 "Membrane Leak Detection System."

        - Coordination of Inspection: Cooperate with testing agency.  Allow access to work areas and staging.  Notify testing agency in writing of schedule for Work of this Section to allow sufficient time for testing and inspection.

          - Do not cover Work until testing and inspection is completed and accepted.

        - Reporting:  Forward written inspection reports to the Architect within 10 working days of the inspection and test being performed.

        - Correction of Work:  Correct deficient applications not passing tests and inspections, make necessary repairs, and retest as required to demonstrate compliance with requirements.

      - CLEANING AND PROTECTING

        - Clean spills, stains, and overspray resulting from application utilizing cleaning agents recommended by manufacturers of affected construction.  Remove masking materials.

        - Protect waterproofing from damage from subsequent work.  Protect waterproofing materials from exposure to UV light for period in excess of that acceptable to waterproofing manufacturer; replace overexposed materials and retest.

END OF SECTION