Tremco, Inc. Commercial Sealants and Waterproofing

Section 07 13 00 SHEET APPLIED WATERPROOFING SYSTEM
TREMproof® 560A

TREMproof 560A is a self-adhesive waterproofing membrane specifically designed for below grade waterproofing. The membrane is composed of SBS modified bitumen with a tri-laminated woven polyethylene facer. A silicone release paper protects the adhesive side of the membrane.

Basic Uses

Designed for use on poured concrete and CMU backfilled walls.

Can be used in conjunction with NUDURA® Insulated Concrete Forms.

Can be used in conjunction with TREMDrain® Series Drainage Mats and select Tremco® protection courses.

This section is easily edited using several common commercial specification software tools.

We recommend you consult with your Tremco technical representative, who can be contacted through: Tremco, Inc., Commercial Sealants and Waterproofing Division, Beachwood OH; (866) 321-6357; email: techresources@tremcoinc.com; www.tremcosealants.com.

Tremco products appear in the following CSI MasterFormat guide specifications available from Tremco:

• Section 07 01 91 Joint Sealant Rehabilitation and Replacement

• Section 07 13 00 Sheet Applied Waterproofing (TREMproof Amphibia)

• Section 07 14 13.01 Hot Fluid-Applied Waterproofing, Deck (TREMproof 6100)

• Section 07 14 13.02 Hot Fluid-Applied Waterproofing, Vegetated Roof (TREMproof 6100)

• Section 07 14 16.01 Cold Fluid-Applied Waterproofing, Vertical and Deck (TREMproof 250GC)

• Section 07 14 16.02 Cold Fluid-Applied Waterproofing, Vertical (TREMproof 250GC)

• Section 07 14 16.03 Cold Fluid-Applied Waterproofing, Deck (TREMproof 250GC)

• Section 07 14 16.04 Cold Fluid-Applied Waterproofing, Vegetative Roof (TREMproof 250GC)

• Section 07 17 16.01 Dual HDPE/Bentonite Waterproofing System (Paraseal)

• Section 07 17 16.03 Dual HDPE/Bentonite Waterproofing System(Paraseal GM)

• Section 07 17 16.04 Dual HDPE/Bentonite Waterproofing System(Paraseal GM/LG 20-MIL)

• Section 07 17 16.05 Dual HDPE/Bentonite Waterproofing System(Paraseal GM/LG 60-MIL)

• Section 07 18 00.01 Traffic Coatings, Vehicular

• Section 07 18 00.02 Traffic Coatings, Pedestrian

• Section 07 18 00.03 Traffic Coatings, Mechanical Rooms

• Section 07 27 13 Modified Bituminous Sheet Air Barriers, Vapor-Retarding (ExoAir 110)

• Section 07 27 23 Board Product Air Barriers, Vapor Permeable (SECUREROCK ExoAir 430)

• Section 07 27 26.01 Fluid-Applied Membrane Air Barriers, Vapor-Retarding (ExoAir 120)

• Section 07 27 26.02 Fluid-Applied Membrane Air Barriers, Vapor Permeable (ExoAir 220)

• Section 07 27 26.03 Fluid-Applied Membrane Air Barriers, Vapor Permeable (ExoAir 230)

• Section 07 92 00 Joint Sealants

• Section 08 85 00 Glazing Sealants

• Section 32 13 73 Concrete Paving Joint Sealants

This document includes Specifier notes in hidden text. To view hidden text, www.bim.net/displaying-hidden-text-in-microsoft-word-step-by-step-instructions-for-windows-and-mac/

Paraseal®, TREMproof®, ExoAir®, Spectrem®, Tremflex®, Dymonic®, Dymeric®, and Proglaze® are registered trademarks of Tremco, Inc.

SECUREROCK® is a registered trademark of United States Gypsum Company. AMPHIBIA™ is a trademark of Volteco S.p.A.
This document is Copyright© 2014 by Tremco, Inc.

SECTION 07 13 00 – SHEET WATERPROOFING

- GENERAL

      - RELATED DOCUMENTS

        - Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this section.

      - SUMMARY

        - Section Includes:

          - Sheet Waterproofing

          - Molded sheet drainage panels

Specifier: If retaining this optional Related Requirements Article, edit to include only those sections included in project manual.

      - REFERENCE STANDARDS

Specifier: If retaining this optional References Article, edit to include only those references cited in the edited section.

        - References, General: Versions of the following standards current as of the date of issue of the project apply to the Work of this Section.

        - ASTM International (ASTM): www.astm.org:

          - ASTM D822 - Standard Practice for Filtered Open-Flame Carbon-Arc Exposures of Paint and Related Coatings

          - ASTM D570 - Standard Test Method for Water Absorption of Plastics

          - ASTM E96 - Standard Test Methods for Water Vapor Transmission of Materials

          - ASTM C1305 - Standard Test Method for Crack Bridging Ability of Liquid-Applied Waterproofing Membrane

          - ASTM D5385 - Standard Test Method for Hydrostatic Pressure Resistance of Waterproofing Membranes

          - ASTM D1000- Standard Test Methods for Pressure-Sensitive Adhesive-Coated Tapes Used for Electrical and Electronic Applications

        - U. S. Environmental Protection Agency (EPA): www.epa.gov.

      - ADMINISTRATIVE REQUIREMENTS

        - Preinstallation Conference: Conduct conference at Project Site.

          - Review requirements for waterproofing products and installation, including surface preparation, substrate conditions, project and manufacturer's details, installation procedures, mockups, testing and inspection requirements, protection and repairs, and coordination and sequencing of waterproofing installation with work of other Sections.

      - ACTION SUBMITTALS

        - Product Data: For each type of waterproofing product specified, including:

          - Include construction details, material descriptions, and tested physical and performance properties of waterproofing.

          - Include manufacturer's written instructions for evaluating, preparing, and treating substrate.

        - LEED Submittals:

          - Product Certificates for Credit MR 5:  For products and materials required to comply with requirements for regional materials, certificates indicating location of material manufacturer and point of extraction, harvest, or recovery for each raw material.  Include statement indicating distance to Project, cost for each regional material, and fraction by weight that is considered regional.

        - Shop Drawings: Show locations for waterproofing system components. Show details for each type of substrate, joints, corners, and edge conditions, including flashings, counter-flashings, penetrations, transitions, and terminations.

        - Samples:  For each exposed product and for each color and texture specified, including the following products:

          - 4-by-4-inch (100-by-100-mm) square of drainage panel.

      - INFORMATIONAL SUBMITTALS

        - Qualification Data: For Installer.

        - Warranty: Sample of special warranties.

        - Field quality control reports.

      - QUALITY ASSURANCE

        - Installer Qualifications: An entity that employs installers and supervisors who are trained and approved by waterproofing manufacturer.

        - Mockups:   Build mockups to verify selections made under Sample submittals and to set quality standards for installation.

          - Build for each typical waterproofing installation including accessories to demonstrate surface preparation, crack and joint treatment, corner treatment, and protection.

            - Size:  As shown on Drawings.

            - Description:  Each type of wall installation.

          - Approval of mockups does not constitute approval of deviations from the Contract Documents contained in mockups unless Architect specifically approves such deviations in writing.

          - Subject to compliance with requirements, approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

      - FIELD CONDITIONS

        - Environmental Limitations:  Apply waterproofing within the range of ambient and substrate temperatures recommended by waterproofing manufacturer.

          - Do not apply waterproofing in snow, rain or fog.

        - Maintain adequate ventilation during preparation and application of waterproofing materials.

      - DELIVERY, STORAGE AND HANDLING

        - Accept materials on site in manufacturer's unopened original packaging.

        - Store products in weather protected environment, clear of ground and moisture, within temperature ranges recommended by waterproofing manufacturer.

Specifier: Retain first option in "Construction Waste" Paragraph below for LEED projects; retain second option for other projects.

        - Construction Waste: Store and dispose of packaging materials and construction waste in accordance with requirements of Division 01 Section ["Construction Waste Management"] ["Temporary Facilities and Controls."]

      - SCHEDULING

        - Schedule work so waterproofing applications may be inspected prior to concealment.

      - WARRANTY

        - Manufacturer's Warranty:  Manufacturer's standard materials-only warranty in which manufacturer agrees to furnish replacement waterproofing material for waterproofing that does not comply with requirements or that fails to remain watertight within specified warranty period.

          - Warranty Period:  ____ years from date of Substantial Completion.

        - Installer's Special Warranty:  Specified form, signed by Installer, covering Work of this Section, for warranty period of ___ years.

          - Warranty includes removing and reinstalling protection board and drainage panels,

- PRODUCTS

      - MATERIALS, GENERAL

        - Source Limitations: Provide waterproofing system materials and accessory products from a single-source system manufacturer.

      - PERFORMANCE REQUIREMENTS

        - General: Waterproofing system shall be capable of performing as a continuous watertight installation and as a moisture drainage plane transitioned to adjacent flashings and discharging water to the building exterior. Waterproofing shall accommodate normal substrate movement, construction material transitions, opening transitions, penetrations, and perimeter conditions without resultant moisture deterioration.

        - Compatibility: Provide waterproofing system materials that are compatible with adjacent materials under conditions of service and substrates on which product is applied, as recommended by waterproofing manufacturer based on testing and field experience.

      - SHEET WATERPROOFING

Specifier: Tremco's Paraseal includes an integral HDPE membrane protective facing.

Specifier: Tremco's Paraseal LG includes an integral HDPE membrane protective facing plus an additional protective laminate layer of spun polypropylene for use in horizontal and vertical applications over lagging on blindside walls, below-slab, and for shotcrete applications.

          - Self-adhesive waterproofing membrane specifically designed for below grade waterproofing. The membrane is composed of SBS modified bitumen with a cross-laminated, non-perforated polyethylene facer.

          - Products:  Subject to compliance with requirements, provide the following:

            - Basis of Design Product: Tremco, Inc., TREMproof 560A

          - Physical Properties:

            - Thickness: 60 mil (1.5 mm)

            - Dimensions: 39” x 67’ (1 x 20.4 m)

            - Surface: Cross laminated polyethylene

            - Service Temperature: -4°F to 167°F (-20°C to 75°C)

            - Application Temperature, 41°F to 113°F (5°C to 45°C)

            - Tensile strength, MD/CD, ASTM D822: 45/48 N/mm2

            - Elongation(Film), (MD/CD), ASTM 822: 230%/200%

            - Low Temperature Flexibility, ICC AC 48: Pass

            - Water Absorption, ASTM D570: <0.1

            - Water Vapor Permeance, ASTM E96: Procedure B:<0.01 perm

            - Crack cycling, 100 cycles, @ -26 °F (-32°C),), ASTM C1305: Pass

            - Resistance to hydrostatic head, ASTM D5385: Pass

            - Adhesion to Primed Concrete, ASTM D1000: 7lbs/inch

Specifier: Tremco's Deckseal has transparent HDPE membrane protective facing for use on elevated horizontal surfaces where flood-testing is required; use with waterproof seam tape.

      - ACCESSORY MATERIALS

        - General:  Furnish accessory materials recommended by waterproofing manufacturer for intended use and compatible with sheet waterproofing.

        - Surface Primer: Solvent based primer used specifically for self-adhered membranes. Primer is composed of a blend of natural resins and solvent/synthetic rubber; may be spray or roller applied

            - Basis of Design Product – Tremco, Inc.; TREMprime 500

        - Termination Bar: Extruded-aluminum or formed-stainless-steel bars with upper flange to receive sealant.

            - Basis of Design Product – Tremco, Inc.; Paraterm Bar

        - Joint Sealants: Termination Seals:

          - Single component, high performance, medium-modulus, low-VOC, UV-stable, non-sag polyurethane sealant.

            - Basis of Design Product: Tremco, Inc.; Dymonic 100.

          - Single component, thermoplastic elastomer sealant.

            - Basis of Design Product: Tremco, Inc.; Tremco 830.

Specifier: Select drainage panel from among eight types listed below in consultation with soils engineer based upon subsurface water conditions and application.

      - WATERPROOFING PROTECTION AND DRAINAGE PANELS

        - Protection Course: Not required.

Specifier: Tremco TREMDrain drainage panel is for general use at backfilled and blindside wall locations.

        - Nonwoven-Geotextile-Faced, Molded-Sheet Drainage Panel: Manufactured composite subsurface drainage panels consisting of a nonwoven, spun-bonded polypropylene facing laminated to one side of a studded, non-biodegradable, polystyrene drainage core.

          - Basis of Design: Tremco, TREMDrain.

          - Flow Capacity, per unit width, ASTM D 4716: 12.5 gpm/ft. (155 lpm/m).

          - Flow Rate, ASTM D 4491: 165 gpm/ft2 (6,724 lpm/m2).

          - Apparent Opening Size: No. 70 sieve (210 micron).

          - CBR Puncture, ASTM D 6241: 275 lb. (1,220 N).

          - Core Compressive Strength, ASTM D 1621: 11,000 lb/ft2 (527 kN/m2).

          - Thickness: 0.25 inch (6.35 mm).

Specifier: Tremco TREMDrain 1000 drainage panel is for use at backfilled and blindside wall and underslab locations requiring a higher compressive strength core or greater flow capacity. It is available with an optional polymeric film backer ( "PF").

        - Nonwoven-Geotextile-Faced, Molded-Sheet Drainage Panel: Manufactured composite subsurface drainage panels consisting of a nonwoven, spun-bonded polypropylene facing laminated to one side of a studded, non-biodegradable, polystyrene drainage core[, with polymeric film attached to back of drainage core].

          - Basis of Design: Tremco, TREMDrain [1000] [1000 PF].

          - Flow Capacity, per unit width, ASTM D 4716: 18 gpm/ft. (224 lpm/m).

          - Flow Rate, ASTM D 4491: 165 gpm/ft2 (6,724 lpm/m2).

          - Apparent Opening Size: No. 70 sieve (210 micron).

          - CBR Puncture, ASTM D 6241: 275 lb (1,220 N).

          - Core Compressive Strength, ASTM D 1621: 15,000 lb/ft2 (718 kN/m2).

          - Thickness: 0.437 inch (11 mm).

Specifier: Tremco TREMDrain 2000 three-layer drainage panel is for use at split slabs and planters requiring a higher compressive strength core or greater flow capacity. It includes a polymeric film backer.

        - Drainage Panel: Manufactured composite subsurface drainage panels consisting of a nonwoven, spun-bonded polypropylene facing laminated to one side of a studded, non-biodegradable, polystyrene drainage core, with polymeric film attached to back of drainage core.

          - Basis of Design: Tremco, TREMDrain 6000/6000PF.

          - Flow Capacity, per unit width, ASTM D 4716: 18 gpm/ft. (223 lpm/m).

          - Flow Rate, ASTM D 4491: 150 gpm/ft2 (6,113 lpm/m2).

          - Apparent Opening Size: 70 sieve (210 micron).

          - CBR Puncture, ASTM D 6241: 320 lb (1,410 N).

          - Core Compressive Strength, ASTM D 1621: 15,000 lb/ft2 (718 kN/m2).

          - Thickness: 0.40 inch (10 mm).

Specifier: Tremco TREMDrain GS 0.5 inch thick three-layer drainage panel is for use at planters. It includes a polymeric film backer; the core also functions as a water retention layer. GS mats are available with optional copper hydroxide-treated root control polymeric film to help control aggressive plant root structures.

Specifier: Tremco TREMDrain GS 1.0 inch thick three-layer drainage panel is for use at planters. It includes a polymeric film backer; the core also functions as a water retention layer. GS mats are available with optional copper hydroxide-treated root control polymeric film to help control aggressive plant root structures. Below has higher flow capacity than above.

Specifier: Tremco TREMDrain TotalDrain is a two-layer drainage panel with high-profile drainage section for water collection and flow around the structure plus a transition section to connect to other TREMDrain panels, for use on backfilled walls and blindside walls.

        - Nonwoven-Geotextile-Faced, Molded-Sheet Drainage Panel: Manufactured composite subsurface drainage panels consisting of a nonwoven, needle-punched polypropylene facing laminated to one side of a studded, non-biodegradable, polystyrene drainage core.

          - Basis of Design: Tremco, TREMDrain TotalDrain.

          - Flow Capacity, per unit width, ASTM D 4716: 21 @ HG= 0.1, 261@HG=0.1

          - Flow Rate, ASTM D 4491: 150 gpm/ft2 (6,113 lpm/m2).

          - Apparent Opening Size: 70 sieve (210 micron).

          - CBR Puncture, ASTM D 6241: 320 lb (1,410 N).

          - Core Compressive Strength, ASTM D 1621: 9,500 lb/ft2 (455 kN/m2).

          - Thickness: 0.437 inch (11 mm), 1 inch (25mm).

Specifier: Tremco TREMDrain TotalDrain High Profile is a two-layer drainage panel with high-profile drainage section for water collection and flow around the structure plus a transition section to connect to other TREMDrain panels, for use on backfilled walls and blindside walls. Below has higher flow capacity than above.

- EXECUTION

      - EXAMINATION

        - Surface Condition: Before applying waterproofing materials, examine substrate conditions.

        - Proceed with installation once unsatisfactory conditions have been corrected.

      - INTERFACE WITH OTHER WORK

        - Sequencing of Work: Coordinate sequencing of waterproofing installation with work of other sections that form portions of building envelope moisture control to ensure that flashings and transition materials can be properly installed and inspected.

        - Subsequent Work: Coordinate waterproofing installation with work of other sections installed subsequent to waterproofing to ensure complete inspection of installed waterproofing and sealing of waterproofing penetrations necessitated by subsequent work.

      - PREPARATION

        - Clean, prepare, and treat substrates. Fill voids with cement grout as recommended by manufacturer.

        - Formed Concrete Surfaces: Remove fins and projections. Fill voids, form-tie holes, and other defects greater than 1/4 inch (6 mm) in depth.

        - Horizontal Concrete Surfaces: Remove standing water, debris, and substances that may impair bonding of patching materials or effectiveness of waterproofing. Fill voids and other defects greater than 1/4 inch (6 mm) in depth.

        - Excavation Support and Protection System: Fill minor gaps and spaces 1 (25 mm) wide or wider with appropriate filling material. Cover or fill large voids and crevices.

      - INSTALLATION, GENERAL

        - Install waterproofing and accessories according to manufacturer's written instructions.

          - The substrate must be clean, dry and free of dust, grease or other contaminant.

          - TREMprime 500 may be applied with a paint brush, roller or sprayer on metal, concrete, wood or polystyrene surfaces as well as on gypsum plasterboard. Average coverage: 0.1 to 0.3 L/m² (0.25 to 0.75 gal US/100 ft²).

          - On backfilled walls, TREMproof 560A can be applied vertically or horizontally. TREMproof 560A membrane shall be lapped onto previous sheet a minimum of 3" (76 mm) as per the markings on the edges of the membrane, and all horizontal laps should be properly shingled a minimum of 3" (76 mm).

          - TREMproof may lap onto horizontal surfaces and terminate. If application consists of full horizontal membrane coverage consult your Tremco Representative.

          - TREMproof 560A must be mechanically roll pressed with a J-Roller to ensure the membrane develops sound contact to the substrate.

          - When required, treat seams with Dymonic 100 or TREMproof 260, lapping minimum 1” (25 mm) onto each sheet of TREMproof 560A while maintaining 1/16” (1.5 mm) thickness of Dymonic 100 or TREMproof 260.

          - A termination bar may be used, when required to, at grade. To terminate the membrane at the base, carry membrane min 6” onto footer. If logistical conditions arise that prevent this contact your Tremco Representative for appropriate termination detail.

        - Protect waterproofing from damage during construction. Repair punctures, tears, and cuts.

Specifier: Retain installation articles and paragraphs that correspond to Project scope of work; delete all others.

      - DRAINAGE PANEL INSTALLATION

        - Place and secure drainage panels in accordance with manufacturer’s written instructions. Use adhesives that do not penetrate waterproofing. Lap edges and ends of geotextile to maintain continuity. Protect installed molded-sheet drainage panels during subsequent construction.

Retain subparagraph below if board insulation is installed before installing molded-sheet drainage panels.

        - Insulation: Refer to Section 07 20 00 "Thermal Insulation."

      - FIELD QUALITY CONTROL

        - Testing Agency: [Owner will] [Contractor shall] engage a qualified testing agency to inspect substrate conditions, surface preparation, waterproofing application, protection, and drainage components, and to furnish reports to Architect.

Retain one of two of the following testing Paragraphs.

Retain "Flood Testing" Paragraph below for elevated horizontal concrete slabs with HDPE membrane installed on top of waterproof membrane. Seams should be taped or otherwise sealed according to manufacturer's written instructions prior to flood testing.

        - Reporting: Forward written inspection reports to the Architect of the inspection and test being performed.

        - Correction: Correct deficient applications not passing tests and inspections, make necessary repairs, and retest as required to demonstrate compliance with requirements.

      - CLEANING AND PROTECTING

        - Protect TREMproof 560A membrane from damage prior to concrete placement.

- END OF SECTION